## Slide 1
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
Performance Study of a Highly Efficient FeS2 Based Thin‑film Solar Cell Using CuBi2O4 as a Back Surface Field Layer
Exam Roll No.: 70406
Registration No.: 2013-012-407
Session: 2019-2020
Presented by

## Slide 2
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
2
CONTENTS
Thin Film Solar Cell (TFSC)
Ferrous Sulphide (FeS2)
Back Surface Field & Buffer Layer
Proposed Structure
Material & Methodology
Algorithm
Structure Optimization
Result & Discussion
Conclusion & Future Works
Reference

## Slide 3: THIN-FILM SOLAR CELL (TFSC)
CdTe, CIGS, CZTS etc. as an absorber in TFSC have emerged as the most attractive materials for photovoltaic technology.
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
3
ADVANTAGES:
High efficiency
Fabrication compatibility
Thermal Stability
Suitable Energy gap
Traditional absorber materials in TFSCs still face issues.
PROBLEMS:
Scarcity of resources
High cost of material processing
High cost of device fabrication
Toxicity
Figure 1: Typical TFSC with different Layer [1].

## Slide 4
PROPERTIES:
High absorbance (105 cm-1, hv > 1.3 eV)
Lattice constant of 5.416 Å
Narrow bandgap of 0.8-0.95 eV
Abundant and Non-toxic
Deposition technique: Sulfurization, Sputting, MBE, CVD, Spin Coating [2].
Figure 2: Crystal Structure of FeS2 [2].
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
FERROUS SULPHIDE (FeS2)
1/11/2026
4
FeS2 can be one of the ideal candidate as an absorber layer in TFSC
( it is also called as “Fool’s Gold” )

## Slide 5
Figure 3: Price Comparison of Various PV Materials [3].
Energy for Extraction: 24 kWh/kg for Si vs 2 kWh/kg for FeS2
Cost of Extraction: $1.70 per kg for Si vs $0.03 per kg for FeS2 [3]
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
FERROUS SULPHIDE (FeS2)
1/11/2026
5
“LOW PRODUCTION COST”
(Most Attractive Feature of FeS2)

## Slide 6
LIMITATION :
Low Open-circuit Voltage (Voc) that does not exceed 200 mV or ∼20% of its band gap leading to a practical efficiency of ~3% [2]
REASONS:
Sulphur vacancies caused by the S dimer (S-S bond length)
Bulk or near surface Non-stoichiometry
Mid gap defects
Thermionic-field emission and Large Dark Current
Metallic like sulfur layer
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
FERROUS SULPHIDE (FeS2)
1/11/2026
6

## Slide 7
CuBi2O4 (Back Surface Field Layer)
PROPERTIES:
Lattice constant of 5.814 Å
Energy band gap of 1.4 to 1.8 eV
Optical absorption coefficient of > 104 cm-1
Non-toxic
Deposition technique: Hydrothermal Synthesis, Pulsed Laser Deposition, CVD, MBE, Spin-coating etc. [4]
GaAs (Buffer Layer)
PROPERTIES:
Lattice constant of 5.653 Å
Energy band gap of 1.424 eV
Non-toxic
High-efficiency
Low cost solar cells
Deposition technique: Sputting, MBE, CVD, Spin Coating etc. [5]
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
7
BACK SURFACE FIELD & BUFFER LAYER

## Slide 8: PROPOSED STRUCTURE
Back Surface Field (BSF) Layer
Anti-reflection Coating
Front Contact
Glass
Mo
CuBi2O4
FeS2
GaAs
FTO
Al
Back Contact
Buffer Layer
Absorber Layer
Substrate
Figure 4: Proposed Structure FeS2/CuBi2O4 Based Dual Heterojunction Solar Cell.
Figure 5: Band diagram of Proposed FTO/GaAs/FeS2/CuBi2O4 Structure.
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
8
CuBi2O4
FeS2
GaAs
FTO
Depletion Region

## Slide 9: MATERIALS & METHODOLOGY
SCAPS-1D (SOLAR CELL CAPACITANCE SIMULATOR)
FEATURES:
Editable effects and properties of materials
Use of sophisticated equations
Optimization of TFSC
Better description of generation and recombination processes
Real-time band diagram.
Analysis of Different types of defect levels
A variety of standard and other spectra etc
Figure 6: Layer Editing Panel.
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
9

## Slide 10: ALGORITHM
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
10
Design & Propose FeS2 based solar cell from reviewing literatures
Develop & Validate the model with published experimental data
Launch SCAPS 1D, Set problem, Provide input parameters & Run the program
is the Device Working?
Analyze data & Draw conclusions
Troubleshoot & Check all Steps
Optimize proposed model
Yes
No

## Slide 11: STRUCTURE OPTIMIZATION: THICKNESS
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
11
JSC and VOC are almost invariant with the change of thickness of CuBi2O4 for every FeS2 layer.
JSC increases with the increment of thickness of FeS2 and becomes constant.
VOC decreases with increment of thickness of FeS2.
Figure 7: Effect on (a) JSC, (b) VOC with the variation of thickness of CuBi2O4 for FeS2 layers.

## Slide 12: STRUCTURE OPTIMIZATION: THICKNESS
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
12
Both FF and ɳ increase sightly with the decrement of thickness of CuBi2O4.
FF first decreases and then increases with increment of thickness of FeS2.
ɳ first increases and then slightly decreases with increment of thickness of FeS2.
Figure 8: Effect on (c) FF and (d) ɳ with the variation of thickness of CuBi2O4 for FeS2 layers.

## Slide 13: STRUCTURE OPTIMIZATION: DOPING CONCENTRATION
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
13
JSC and VOC increase with the increment of doping concentration of CuBi2O4
JSC and VOC increase sightly with the increment of doping concentration of FeS2
Figure 9: Effect on (a) JSC, (b) VOC with the variation of Doping Concentration of CuBi2O4 for FeS2 layers.

## Slide 14: STRUCTURE OPTIMIZATION: DOPING CONCENTRATION
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
14
FF and ɳ increase with the increment of doping concentration of CuBi2O4
FF and ɳ first remain constant with the increment of doping concentration of FeS2
Figure 10: Effect on (c) FF and (d) ɳ with the variation of Doping Concentration of CuBi2O4 for FeS2 layers.

## Slide 15: STRUCTURE OPTIMIZATION
Material | Thickness (μm)
GaAs | 0.1
FeS2 | 0.8
CuBi2O4 | 0.2
Material | Donor Doping Density (cm-3) | Acceptor Doping Density (cm-3)
GaAs | 1018 | 0
FeS2 | 0 | 1017
CuBi204 | 0 | 3.7×1018
Table 2: Optimum Doping Profile for Proposed Structure.
Table 1: Optimum Layer Thickness for Proposed Structure.
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
15

## Slide 16: RESULT & DISCUSSION
Figure 5.13: J-V Characteristics of Optimal Structure.
Figure 5.3: Spectral Response of Optimal Structure.
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
16
Open Circuit Voltage increases significantly in proposed dual heterojunction structure.
Quantum Efficiency also increases significantly in proposed dual heterojunction structure.

## Slide 17: RESULT & DISCUSSION
Table 3: Device performance of the optimized FeS2 based solar cells.
PARAMETERS | FeS2 Absorber Layer | FeS2/CuBi2O4 Absorber Layer | Percentage of Increment
Short Circuit Current Density, Jsc (mA/cm2) | 46.349 | 49.64 | 7.1
Open Circuit Voltage, Voc (V) | 0.517 | 0.8426 | 63.67
Fill Factor, FF (%) | 79.58 | 80.0242 | 0.5581
Efficiency, η (%) | 19.1881 | 33.29 | 73.493
Max. Voltage, Vmmp (V) | 0.442 | 0.703 | 59.049
Max. Current, Jmmp (mA/cm2) | 43.391 | 47.355 | 9.13
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
17

## Slide 18: RESULT & DISCUSSION
Table 4: Performance of the proposed solar cell in comparison with other solar cells.
No. | Thin Film Solar Cell | VOC (V) | JSC (mA/cm2) | FF (%) | PCE (%) | Type
1. | Si (crystalline) | 0.705 | 42.7 | 82.8 | 25.0 | Experimental
2. | Si (multi-crystalline) | 0.664 | 37.7 | 78.9 | 20.3 | Experimental
3. | CIGS | 0.734 | 39.58 | 80.40 | 23.84 | Experimental
4. | Perovskite | 1.18 | 25.14 | 84.8 | 25.20 | Experimental
5. | CdTe | 0.887 | 31.69 | 78.50 | 22.10 | Experimental
6. | CZTS | 0.716 | 33.7 | 80.3 | 19.4 | Experimental
7. | FeS2 | 0.842 | 49.64 | 80.0242 | 33.29 | Theoretical
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
18

## Slide 19: CONCLUSION & FUTURE WORKS
FUTURE WORKS
In future different materials can be investigated as BSF for increasing the efficiency.
The proposed model may be fabricated in the Laboratory in future.
P-I-N structured FeS2 may be designed and simulated which is unexplored.
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
19
CONCLUSION
Various defects like interface defect, surface recombination etc. will minimize the efficiency.
If 70-80% of simulated result can be found that will be a breakthrough.
FeS2 can be used as best candidate for absorber using a suitable BSF layer with suitable band alignment.

## Slide 20: REFERENCE
[1] F. Baig, Y.H. Khattak, S. Ullah, B.M. Soucase, S. Beg, H. Ullah, Numerical analysis a guide to improve the efficiency of experimentally designed solar cell, Appl. Phys. A. 124 (2018) 471. doi:10.1007/s00339-018-1877-x.
[2] Limpinsel, M., Farhi, N., Berry, N., Lindemuth, J., Perkins, C.L., Lin, Q., and Law, M. (2014). An inversion layer at the surface of n-type iron pyrite. Energy Environ. Sci. 7,
1974.
[3] Caba´ n-Acevedo, M., Kaiser, N.S., English, C.R., Liang, D., Thompson, B.J., Chen, H.E., Czech, K.J., Wright, J.C., Hamers, R.J., and Jin, S. (2014). Ionization of high-density deep donor defect states explains the low photovoltage of iron pyrite single crystals. J. Am. Chem. Soc. 136, 17163–17179.
[4] Wang, F.; Septina, W.; Chemseddine, A.; Abdi, F. F.; Friedrich, D.; Bogdanoff, P.; van de Krol, R.; Tilley, S. D.; Berglund, S. P. Gradient Self-Doped CuBi2O4 with Highly Improved Charge Separation Efficiency. J. Am. Chem. Soc. 2017, 139 (42), 15094− 15103.
[5] J. Yin et al., “Charge redistribution at GaAs/P3HT heterointerfaces with different surface polarity,” J. Phys. Chem. Lett., vol. 4, no. 19, pp. 3303–3309, 2013.
[6] Ennaoui, A., Fiechter, S., Pettenkofer, C., Alonso-Vante, N., Bu¨ ker, K., Bronold, M.,
Ho¨ pfner, C., and Tributsch, H. (1993). Iron disulfide for solar energy conversion. Sol. Energy Mater. Sol. Cells 29, 289–370. 2. Ennaoui, A., and Tributsch, H. (1984). Iron sulphide solar cells. Sol. Cells 13, 197–200.
[7] Hossain, J., Mondal, B.K. and Mostaque, S.K., 2021. Design of a highly efficient FeS2-based dual-heterojunction thin film solar cell. International Journal of Green Energy, pp.1-12.
[8] Hosen, A., Mian, M. and Ahmed, S.R.A., 2021. Simulating the performance of a highly efficient CuBi2O4-based thin-film solar cell. SN Applied Sciences, 3(5), pp.1-13.
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
20

## Slide 21
THANK YOU
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
21

## Slide 22
Q & A
Department of Electrical and Electronic Engineering
Faculty of Engineering and Technology
University of Dhaka
1/11/2026
22